- Polystyrene Resin EA3300

- Technical datasheet (TDS)

| Items | Test Method | Unit | Nominal Value |
| --- | --- | --- | --- |
| Melt Mass-Flow Rate(MFR) | ASTM D1238 | g/10min | 1.7 |
| Notched Izod Impact Strength (1/8in) | ASTM D256 | J/m | 19.0 |
| Notched Izod Impact Strength (1/4in) | ASTM D256 | J/m | 16.4 |
| Tensile Strength (Yield) | ASTM D638 | MPa | 55 |
| Tensile Strength (Break) | ASTM D638 | MPa | 55 |
| Tensile Elongation at Break | ASTM D638 | % | 4.5 |
| Tensile Modulus | ASTM D638 | MPa | 3381 |
| Flexural Strength | ASTM D790B | MPa | 83 |
| Flexural Modulus | ASTM D790B | MPa | 3174 |
| Distortion Temperature | ASTM D648 | °C | 92 |
| Vicat Softening Temperature | ASTM D1525 | °C | 109 |
| Density | ASTM D792 |  | 1.04 |
| Flammability | UL94 |  | 94HB |

Note: These are typical properties only and not to be construed as specifications. Users should confirm results by their own tests.

Product property and applications

With the advantage of high grade of transparency, superhigh molecular weight, and low residual, the transparent GPPS EA3300 has good performance in its appearance and applications. It’s especially suitable for biaxial tension package for food and other similar products. The internal transparent parts in refrigerator made by EA3300 have better performance in tenacity.

FDA Certificate

GPPS EA3300 confirms to regulations 21CFR177.1640 for food additive in FDA. Your products can be used safely in food utensils.

UL Certificate

GPPS EA3300 confirms to UL certificate and can be used in electronics industry.

Safety operation instruction

GPPS EA3300 resin is low toxicity. It can be used in general conditions and is not harmful for eyes, skin, respiratory and digestive system. Please avoid inhalation once dust and vapour generates. In case any other material mixes with GPPS, please contact our sales or technical delegate asking for MSDS and comply with safety instructions.