Polystyrene Resin MC3100

Technical datasheet (TDS)

| Items | Test Method | Unit | Nominal Value |
| --- | --- | --- | --- |
| Melt flow rate (MFR) | ASTM D1238 | g/10min | 3.0 |
| Notched Izod Impact Strength (1/8in) | ASTM D256 | J/m | 19 |
| Notched Izod Impact Strength (1/4in) | ASTM D256 | J/m | 14 |
| Tensile Strength (Yield) | ASTM D638 | MPa | 54 |
| Tensile Strength (Break) | ASTM D638 | MPa | 54 |
| Tensile Elongation at Break | ASTM D638 | % | 4.5 |
| Tensile Modulus | ASTM D638 | MPa | 3381 |
| Flexural Strength | ASTM D790B | MPa | 83 |
| Flexural Modulus | ASTM D790B | MPa | 3105 |
| Distortion Temperature | ASTM D648 | °C | 91 |
| Vicat Softening Temperature | ASTM D1525 | °C | 108 |
| Density | ASTM D792 |  | 1.04 |
| Flammability | UL94 |  | 94HB |

Note: These are typical properties only and not to be construed as specifications. Users should confirm results by their own tests.

Product property and applications

With the good advantage of injection and extrusion, products made by GPPS MC3100 have good performance of high transparency, good heat resistance and abrasive resistance. It’s suitable for transparent packing box, foamed sheets, decorating blocks, and toys.

FDA Certificate

GPPS MC3100 confirms to regulations 21CFR177.1640 for food additive in FDA. Your products can be used safely in food utensils.

UL Certificate

GPPS MC3100 confirms to UL certificate and can be used in electronics industry.

Safety operation instruction

GPPS MC3100 resin is low toxicity. It can be used in general conditions and is not harmful for eyes, skin, respiratory and digestive system. Please avoid inhalation once dust and vapour generates. In case any other material mixes with GPPS, please contact our sales or technical delegate asking for MSDS and comply with safety instructions.