- High Impact Polystyrene Resin MA5210

- Technical datasheet (TDS)

| Items | Test Method | Unit | Nominal Value |
| --- | --- | --- | --- |
| Melt Mass-Flow Rate(MFR) | ASTM D1238 | g/10min | 4.0 |
| Notched Izod Impact Strength (1/8in) | ASTM D256 | J/m | 120 |
| Notched Izod Impact Strength (1/4in) | ASTM D256 | J/m | 98 |
| Tensile Strength (Yield) | ASTM D638 | MPa | 32 |
| Tensile Strength (Break) | ASTM D638 | MPa | 28 |
| Tensile Elongation at Break | ASTM D638 | % | 50 |
| Tensile Modulus | ASTM D638 | MPa | 2277 |
| Flexural Strength | ASTM D790B | MPa | 45 |
| Flexural Modulus | ASTM D790B | MPa | 2277 |
| Distortion Temperature | ASTM D648 | °C | 86 |
| Vicat Softening Temperature | ASTM D1525 | °C | 103 |
| Density | ASTM D792 |  | 1.03 |
| Flammability | UL94 |  | 94HB |

Note: These are typical properties only and not to be construed as specifications. Users should confirm results by their own tests.

Product property and applications

With the good advantage of injection molding property and favorable mold ejection property, the products made by HIPS MA5210 shows outstanding performance of rigidity, tenacity, high gloss in surface, and good appearance. This grade is widely used in components and parts for TV sets, air-conditioners, refrigerators, computers, household products, and office stationeries.

- FDA Certificate

HIPS MA52100 confirms to regulations 21CFR177.1640 for food additive in FDA. Your products can be used safely in food utensils.

- UL Certificate

HIPS MA52100 confirms to UL certificate and can be used in electronics industry.

Safety operation instruction

HIPS MA52100 resin is low toxicity. It can be used in general conditions and is not harmful for eyes, skin, respiratory and digestive system. Please avoid inhalation once dust and vapour generates. In case any other material mixes with GPPS, please contact our sales or technical delegate asking for MSDS and comply with safety instructions.